## Slide 1: Introduction to Composite Materials Design Chapter 7: strength
Introduction to Composite Materials Design—Third Edition
Dr. Ever J. Barbero
November 24, 2018

## Slide 2: 7.0. Introduction
Fig. 6.2

## Slide 3: 7.0. Modes of fracture

## Slide 4: 7.0. Review micromechanics
Longitudinal tension:.......
Longitudinal compression:
Transverse tension:………
Transv. compression:
Out-of-plane shear:.......
In-plane shear:………………..

## Slide 5: 7.1.1. Strength ratio
This is for a single lamina! Not for a laminate!
For a laminate we use FPF and LPF defined later.

## Slide 6: 7.1.2. Maximum stress

## Slide 7: 7.1.2. Max. stress, cont’d

## Slide 8: 7.1.3. Max. strain

## Slide 9: 7.1.4. Interacting failure criterion
Longitudinal tensile strength is fiber dominated, thus uncoupled from anything else.
Longitudinal compressive strength is fiber and matrix influenced, so it is coupled (G12 is matrix dominated)

## Slide 10: 7.1.4. Interacting (cont’d)
Matrix dominated strengths:
  Transverse tensile strength F2T
  In-plane shear F6
  Out-of-plane shear F4
Since all three are matrix dominated, they interact!

## Slide 11: 7.1.4. interacting (cont’d)

## Slide 12: 7.2. Laminate First Ply Failure (FPF)

## Slide 13: 7.2. FPF
Use some interacting failure criterion
  R1 = <F1t /s1> + <-F1c /s1>
  R2 = [ - b +/- sqrt { b2 + 4 a } ] / (2a)
Compute the minimum R in each lamina
  R(k)=min(R1, R2, R6) in lamina k
Find the lamina that has the smallest R(k)
  R = min(R(k))
  R is the strength ratio of the whole laminate
If R<1, then the lamina with the min(R) fails.
  The thickness or strength must be increased, or the load decreased
If R>1, R is the safety factor in allowable stress design
Allowable stress design (ASD) is not used any more. Instead, use Load Resistance Factor Design (LRFD) or better reliability analysis.

## Slide 14: FPF (cont’d)
The fact that one lamina fails does not mean the laminate fails unless it is poorly designed
Acceptable design? Start with the 10% rule
  At least 10% thickness of 0-deg
  At least 10% thickness of 90-deg
  At least 10% thickness of +/-45

## Slide 15: 7.2.1. In-situ strength affects FPF
Fig. 7.8

## Slide 16: s2 in [0/90/0] T300/944

## Slide 17: Mode I fracture toughness
Fig. 4.20
Material fails when the Energy released by the growing crack GI
exceeds the energy absorbed by the material to grow a crack GIC
Notes: F2T is the transverse tensile strength of an unconstrained “thick” unidirectional lamina.

## Slide 18: Mode II fracture toughness GIIC
Fig. 4.26
Material fails when the Energy released by the growing crack GII
exceeds the energy absorbed by the material to grow a crack GIIC

## Slide 19: In-situ strength
Transition thickness:
Glass/Epoxy : tt = 0.6 mm
Carbon/Epoxy : tt = 0.8 mm

## Slide 20: Why this happens?

## Slide 21: Recap FPF
Use in-situ strength
Decide what failure criterion you want (or have-to) use
Compute FPF
If the laminate is well designed, FPF is not catastrophic, it just signals the onset of damage
To find the laminate strength, compute the last ply failure (LPF)

## Slide 22: 7.2. Laminate strength (LPF)
Load
FF
FPF
Deformation
B
A
First Ply Fails
Second Ply Fails
Third Ply Fails
Fracture
Intact Laminate
Totally Degraded

## Slide 23: 7.2.1. Ply discount
FPF: compute R@failure with the failure criteria of your choice
Degrade the moduli 
LPF: re-compute R@failure ignoring matrix modes, i.e., LPF corresponds to a fiber mode of failure (LPF is the FPF of the second round of calculations)
0<d<1: damage factor

## Slide 24: Better than ply discount
Chapter 8. Damage

## Slide 25: 7.4. Carpet plots for strength design
Restrict the design space to the following family of laminates:
Strength-design:
Notes: Before teaching this, I go teach 6.4 and 6.5, which I skipped when teaching chapter 6.

## Slide 26: 7.4. FPF tensile strength

## Slide 27: 7.4. LPF tensile strength

## Slide 28: 7.4. LPF compressive strength

## Slide 29: 7.4. LPF shear strength

## Slide 30: Thank you !
Questions ?