## Slide 1: Introduction to Composite Materials Design—3rd Edition
Chapter 6
©2018 by Taylor & Francis Group LLC, all rights reserved. See the front matter of the textbook for copyright information. Do not post electronically outside of course delivery systems where access is strictly restricted to students enrolled in your course.

## Slide 2: Cylindrical pressure vessel

## Slide 3: Plate deformation

## Slide 4: Stress resultants

## Slide 5: Stress and strain in homogeneous plate

## Slide 6: Stress and strain in laminated plate

## Slide 7: Notation used to describe a laminate

## Slide 8: Coupling effects

## Slide 9: Universal carpet plot modulus Ex Glass/Epoxy

## Slide 10: Universal carpet plot vxy E-Glass/Epoxy

## Slide 11: Universal carpet plot Ex Carbon/Epoxy

## Slide 12: Universal carpet plot vxy Carbon/Epoxy

## Slide 13: Universal shear stiffness G and strength F

## Slide 14: Homogeneization

## Slide 15: Membrane design

## Slide 16: Design of a box beam

## Slide 17: Transformed section method

## Slide 18: Thermal expansion

## Slide 19: CTE mismatch